## Slide 1: Wheels and Bearings

## Slide 2: Wheel Materials
Polyurethane
μ-rolling = 0.02-0.04 Acceptable for non-driven
μ-static = 0.2 Insufficient for driven
Rubber
μ-static = 0.35-45 75-125% Improvement

## Slide 3: Bearing Materials
Material | σUTS (MPa) | Brinell Hardness (kg/mm2) | Approximate Cost (£)
Steel: SAE-AISI 52100 | 590-2100 | 180-210 | 15
Titanium: ASTM Grades 7 | 550 | 200 | 25
Ceramic: Silicon Nitride | 170 | 1479 (converted from Vickers’ hardness) | 70-115
Steel and Titanium perform similarly
Titanium favoured due to greater wear and corrosion resistance despite greater cost

## Slide 4: Wheel-Gear Adhesives
Estimated Minimum Tensile Strength Required
Adhesive | Tensile Strength (N/mm2) | FOS | Cost (£/gram) | Cost(£/mm2) | Cost (per wheel)
Weicon GMK 2410 Rubber Metal Contact Adhesive | 0.54 (Steel to SBR Rubber) | 3.6 | 0.124 | 3.72x10^-5 | 0.0954
Cole-Parmer Silicone Rubber Bonding Cement: DOWSIL™ 732 Multi-Purpose Sealant | 2.3 | 15.3 | 0.1367 | 4.101x10^-5 | 0.1052
Loctite Super Glue ULTRA Gel Control | 21.12 (Aluminium to Rubber) | 140.8 | 1.623 | 4.869x10^-4 | 1.249